## Slide 1: Low-Loss Cavities for Advanced Virgo+: From the Stable Recycling Cavities to the Output Mode Cleaner
Ward Amar
Supervised by: Raffaele Flaminio
Co-supervised by: Romain Bonnand
LAPP seminar - 18th of September 2026

## Slide 2: Table of content
Introduction
Stable recycling cavities simulation: projects accomplished
The output mode cleaner losses characterization: project ongoing
Scientific production
Doctoral training followed
Third year plan
The first GW detection mozzaik at the LVK week in Pisa.

## Slide 3: Introduction
Power Recycling Cavity (PRC)
Signal Recycling Cavity (SRC)
Advanced Virgo+ is a gravitational-wave detector based on Michelson interferometry.
Gravitational waves produce extremely small changes in the interferometer arm lengths, of order 10^-18.
Achieving this sensitivity requires recycling high optical power while minimizing optical losses.
Two key optical systems contribute to the loss budget:
  Power & Signal Recycling Cavities (PRC/SRC)
  Output Mode Cleaner (OMC)
Virgo upgrades
  Stable recycling cavities → improve the robustness and optical performance of the PRC/SRC.
  Low-loss OMC → reduce losses at the output of the interferometer.
Output mode cleaner
Notes: Before getting into the measurements, I want to briefly put the work in context.
To reach this level of sensitivity, we need to make very efficient use of the laser light circulating in the interferometer. And this means that optical losses become very important.
There are several places where we have to worry about losses, but in my work I focus on two optical systems: the power and signal recycling cavities, and the output mode cleaner.

## Slide 4: Stable recycling cavities simulations
Short cavities design
   Astigmatism losses
Mirrors surface imperfections
   Requires specifying surface RMS
Radius of Curvature (RoC) manufacturing errors
   RoC errors specifications and correction
Thermal lensing due to the high power storage in the arms
  Study thermal lens compensation method
first year
first year
first year
Power = 236kW
Absorption= 0.5 ppm
Corresponds to 17km spherical lens
Second year

## Slide 5: The output mode cleaner of Advanced Virgo+
The OMC is a bow-tie Fabry-Perot cavity placed at the output of the interferometer.
The output beam of the ITF consists of:
  The TEM00 ( carrier of the GW signal)
  HOMs (noise to the GW signal)
  Modulation sidebands ( for the control of the ITF)
The OMC acts as a filter, when it’s resonant it reflects the HOMs and the modulation sidebands.
Losses in the OMC destroy the squeezed states  increase the quantum noise  limit the detector sensitivity
Transmitted beam
Input beam
Reflected beam
Notes: Reverse the OMC orientation., reflected beam, remove the BS beam.

## Slide 6: The output mode cleaner (OMC) of AdV+
Photo of the OMC set-up at LAPP

## Slide 7: OMC losses characterization set-up at the LAPP
Focusing lenses
Set-up:
How do we keep the OMC resonant?
  Only frequency that matches the cavity resonance frequency can pass (resonate). We want the TEM00 to be resonant.
Two feedback loops keep it stable
  Temperature control: Peltier cells below the OMC adjust its temperature → stabilizes the cavity length.
  Cavity lock: the laser frequency is adjusted to follow the OMC resonance → keeps the laser resonant with the TEM00 mode.
Notes: Control loops with the optical scheme.

## Slide 8: OMC spatial modes
We can change the laser frequency by changing the temperature of the laser crystal.
As we change the laser frequency, we observe different cavity modes
The 23rd-order HOM is the closest higher-order-mode resonance to TEM00
HOM2
TEM00
FSR = 808MHz
HOM1
23rd HOM
Notes: Larger scan and show the 23rd closest

## Slide 9: OMC TEM00 lock and loss calculation
The cavity is locked when the laser is resonant with the TEM00 mode, so the TEM00 power transmitted by the cavity is maximized.
According to the energy conservation law:
We made two measurements of the OMC losses using two different configurations
  First configuration: losses =3.4 % ± 0.1%
  Second configuration: losses =3.5 % ± 0.1%
Transmitted power
Reflected power
Loss
Notes: Show the diffePrent configurations , default and configuration , P_losses/P_in_Pref  Loss
Remove the BS beam. Change the color of Confi2

## Slide 10: Investigation of sources of losses in the OMC
Targeted level of losses in the OMC = 2%
Expected total internal losses ~ 1.4% ± 0.4%
We measured average losses ~ 3.4% ± 0.1%
Several OMCs show excess losses.
Motivation: why there is excess of losses compared to the expected value?
We investigated two possible scattering mechanisms:
  Backscattered light
    Imperfections on the OMC surfaces scatter part of the circulating light back toward the input.
  Rayleigh scattering
    Microscopic density fluctuations inside the fused-silica substrate scatter light out of the cavity.
These scattering mechanisms can introduce more noise into the interferometer.
Notes: OMC losses per squeezing less 1%
Motivation: why there is this excess of losses compared to what we expect and what we want
Explain the sources of scattering.
In addition, these phenomena can introduce more noise by scatter light to the ITF

## Slide 11: Losses due to backscattered light (1/4)
Backscattered light Microscopic imperfections on the OMC surfaces scatter part of the circulating light back toward the input.
    We measured the backscattered light from the OMC using a powermeter
Back-scattered beam
Transmitted beam
Input beam
Backscattered light
Light backscattered ~ 20 ppm  doesn’t explain the excess losses on the OMC.
Reflected beam
Notes: Flip the two, move the omc scheme setup below. Up to down, left to right.
Put the plot in mW
Remove input arrow of the second scheme

## Slide 12: Backscattering for different cavity modes (2/4)
Scanning different longitudinal modes (q) of the OMC shows a change in the backscattered light power and beam shape
We installed a camera to observe the beam shape. We captured interesting images of scattered light
At q=2
At q=1
At q=3
At q=4
At q=5
At q=6
At q=7
At q=8
Notes: Scan , put camera, put more images, explain components 00, 23, 46
pit the scale in nW
Fix the plot from 1-8 and the labels on the images

## Slide 13: Backscattered modes power (3/4)
We took more images for different cavity modes
By analyzing the images of scattered light we can quantify how much power exist in each mode:
The 23rd order mode is showing an alternating pattern, while the TEM00 is not alternating.
23rd order mode power
TEM00 mode power
Cavity mode (q)
Cavity mode (q)
Notes: We plan*
Add slide to show the source of the scattering

## Slide 14: Model of backscattered light (4/4)
Variation of backscattered power is not a surprise if we look closely at the OMC scattering mechanism:
If we assume equal scattering from each surface of the OMC we have two cases:
  Case 1: where all the scattered fields interfere constructively and the backscattered power is maximum
  Case 2: where the scattered fields interfere destructively and the backscattered power is minimum.
While this pattern applies to the 23rd order mode, it doesn’t fully describe the TEM00 behavior.
We plan to extend the measurement to recognize the pattern of the TEM00.
l1
Output
l2
l3
l4
Input
Mirror 2
Mirror 1
Mirror 3
Mirror 4
Notes: Plans to extend the measu. Should come here

## Slide 15
  Losses due to Rayleigh scattering
  Rayleigh scattering of light by molecules in the atmosphere gives the sky its beautiful colors!
  Rayleigh scattering in the fused-silica substrate of the OMC is not as desirable…
Photo taken by my camera during the GW advanced detector workshop in Elba island.

## Slide 16: Losses due to Rayleigh scattering (1/4)
Rayleigh scattering
  Microscopic density fluctuations inside the fused-silica substrate scatter light out of the cavity.
Set- up: Images of the OMC substrate are taken using a CCD camera and a Fujifilm objective.
Input beam
CCD
Objective
Input beam
output beam Power=24.5 mW

## Slide 17: Losses due to Rayleigh scattering (2/4)
The raw images of the OMC for different f#:
  The f# determines the objective aperture diameter.
  The camera doesn’t collect all scattered light only collects the fraction emitted into its observation cone ( solid angle).
  For different f#, we calculate the solid angle.
f# | Ω (sr) | (m.c.) | (nW) | (μW/sr)
1.7 | 28e-4 | 0.932 | 140.5 | 48.82
2.8 | 10e-4 | 0.317 | 66.43 | 62.59
4 | 5.2e-4 | 0.202 | 31.86 | 61.25
5.6 | 2.6e-4 | 0.100 | 16.71 | 64.97
8 | 1.3 e-4 | 0.046 | 8.671 | 66.68
f# | Ω (sr) |  |  | 
1.7 | 28e-4 | 0.932 | 140.5 | 48.82
2.8 | 10e-4 | 0.317 | 66.43 | 62.59
4 | 5.2e-4 | 0.202 | 31.86 | 61.25
5.6 | 2.6e-4 | 0.100 | 16.71 | 64.97
8 | 1.3 e-4 | 0.046 | 8.671 | 66.68
We find the sum of counts on the CCD that correspond to the scattered light.
We convert the number of counts to (W) using the camera calibration.
We calculate the scattered power per solid angle (μW/sr)
Notes: Larger pupil size  larger solid angle  more scattered power collected

## Slide 18: Losses due to Rayleigh scattering (4/4)
The scattered power for vertically polarized beam β=0:
We detect the scattered power at which corresponds to the maximum scattering direction in our set-up.
The maximum scattered power per steradian:
The total scattered power is the integral of over hemisphere
Scattering losses:
  Average losses value = 2.07% ± 0.23% (Preliminary!!)
f# | (μW/sr) | 
1.7 | 48.82 | 408.98
2.8 | 62.59 | 524.35
4 | 61.25 | 513.16
5.6 | 64.97 | 527.52
8 | 66.68 | 558.61
f# |  | 
1.7 | 48.82 | 408.98
2.8 | 62.59 | 524.35
4 | 61.25 | 513.16
5.6 | 64.97 | 527.52
8 | 66.68 | 558.61
polarization
Notes: Remove solid angle and P_cal
Edit the scheme to show the vertical pol
P_sca depends on theta and phi

## Slide 19: Losses budget of the OMC
Sources of losses  loss percentage:
  Absorption losses of the substrate:
  Absorption losses in the coatings:
  Scattering by surfaces: measured by LMA,
  HR mirror residual transmission :
  Rayleigh scattering: measured (expected[1]: 0.55%± 0.02%)
  Total losses =
Reminder: we have measured internal losses ~ 3.4% 0.1%
The results of the loss source are preliminary and we are still investigating them!
  [1] Xu Chen, Li Ju, Raffaele Flaminio, Harald Lu ̈ck, Chunnong Zhao, and David G Blair. Rayleigh scattering in fused silica samples for gravitational wave detectors. Optics Communications, 284(19):4732–4737, 2011. 13
Notes: First 3 sources are measured by LMA
Reference to the paper.

## Slide 20: Scientific production
Technical notes and paper:
Virgo note: Thermal lenses' impact on the stable recycling cavities of AdV+, Virgo technical note VIR-0184A-26 (2026).
Virgo note: Losses characterization of the SN5 Output Mode Cleaner at LAPP, Virgo technical note VIR-0589A-26 (2026).
Virgo note: Backscattered light measurements of the SN5 OMC at LAPP, Virgo technical note (2026) (note in preparation).
Vigo note: Multiple mirrors’ flatness impact on the SRC losses (2026). ( note in preparation).
Along with R. Flaminio, R. Bonnand and E. Tournefier, we have submitted a paper about the work we did on the stable recycling cavities optical design. ( in preparation).
Presentations:
Presentation at the JRJC (2025) at Saint-Jacques de la mer: “Non-degenerate low-loss recycling cavities for the gravitational waves detector Virgo (in addition to proceedings)”
Presentation at the Virgo optics group meeting (2026): “Thermal lens impact on the gain of the stable power recycling cavity”
Presentation at the LIGO-Virgo-KAGRA week (2026) at Pisa: “Impact of thermal lenses in the ITM on the stable signal recycling cavity losses and its possible reduction”
Presentation at the Gravitational waves advanced detector workshop - GWADW (2026) at Elba island: “Optical design of stable recycling cavities for the Virgo gravitational wave detector”
Notes: Virgo note* ( paper in preparation)
Title below event
LVK week
GWADW in detail

## Slide 21: Doctoral training followed
Training followed in total:
Type | Name | Hours worked | ADUM status (programmed, validated, awaiting validation...)
Scientific | ED Physique 24-25 : Physics in the XXIst Century | 20 | validated
Transversal | JOURNEE DE RENTREE DES DOCTORANTS 2024 | 4 | validated
Transversal | Cours de français - ACCENTS-Annecy | 40 | validated
Transversal | MOOC Research integrity in scientific professions - Univ. Bordeaux - 24 - 7th edition | 15 | validated
Scientific | MaNiTou summer school – Gravitational waves | 32 | Validated
Professional | MOOC Doctorat et poursuite de carrière/ PhD and career development | 12 | validated
Science communication | Preparation for the UNITA My 3-min PhD thesis competition | 10 | Validated
Total hours |  | 133/120 | 
Chart: 
| Scientific | Transversal | proffesional | Communication
ADUM hours | 52 | 59 | 12 | 10

## Slide 22: Third year plan
Backscattered light study: perform extended measurements of the OMC backscattered light.
Rayleigh scattering: perform tests related to the camera calibration to verify the results.
New alignment set-up for the OMC at the LAPP (if time allows):
  It is a challenge to align and operate the OMC on the TEM00 with the presence of the HOM at the output of the interferometer.
  We plan to test a technique (MDWS): Modulated Differential Wavefront Sensing
    Classic alignment methods​ → mode - dependent
    MDWS  mode - selective
Write the thesis!
Notes: Write if time allows.

## Slide 23: Thank you

## Slide 24: Extra slides

## Slide 25: Losses due to Rayleigh scattering
The scattered power is expressed by:
  In the direction of the observation:
  , , as a result:
  which is the maximum scattered power.
The scattered power per steradian:
The total scattered power is the integral of over the total scattering surface
Scattering losses:
  Average losses value = 2.07% ± 0.23% (Preliminary!!)
f# | (nW) | Ω (sr) | (μW/sr) | 
1.7 | 140.5 | 28e-4 | 48.82 | 408.98
2.8 | 66.43 | 10e-4 | 62.59 | 524.35
4 | 31.86 | 5.2e-4 | 61.25 | 513.16
5.6 | 16.71 | 2.6e-4 | 64.97 | 527.52
8 | 8.671 | 1.3 e-4 | 66.68 | 558.61
f# |  | Ω (sr) |  | 
1.7 | 140.5 | 28e-4 | 48.82 | 408.98
2.8 | 66.43 | 10e-4 | 62.59 | 524.35
4 | 31.86 | 5.2e-4 | 61.25 | 513.16
5.6 | 16.71 | 2.6e-4 | 64.97 | 527.52
8 | 8.671 | 1.3 e-4 | 66.68 | 558.61

## Slide 26: Losses due to Rayleigh scattering (3/4)
The camera does not see all the scattered light. It only collects the fraction emitted into its observation cone.
For different f#:
θ
θ
Entrance pupil diameter:
For small angle approximation:
Solid angle:
Larger pupil size  larger solid angle  more scattered power collected
f# | (mm) | Ω (sr)
1.7 | 20.6 | 28e-4
2.8 | 12.5 | 10e-4
4 | 8.8 | 5.2e-4
5.6 | 6.3 | 2.6e-4
8 | 4.4 | 1.3 e-4
f# |  | Ω (sr)
1.7 | 20.6 | 28e-4
2.8 | 12.5 | 10e-4
4 | 8.8 | 5.2e-4
5.6 | 6.3 | 2.6e-4
8 | 4.4 | 1.3 e-4