## Slide 1
Molecular Modeling of the swelling properties and interlayer structure of Cs- and K- Montmorillonites: Effects of charge distribution in the clay layers
Brice NGOUANA, Ph.D Student
Prof. Andrey KALINICHEV, Supervisor
Radiochemistry Group, Subatech

## Slide 2
Cs 135, Cs 137 isotopes belong to the family of long-lived ( > 30 ans) radioactive waste.
Introduction
Deep geological storage is considered by many countries as the appropriate long term solution for management and storage of this type of radioactive waste.
Composition minéralogique moyenne de la formation du Callovo-Oxfordien
41% clay minerals (interstratified illite-smectite and illite)
31% calcite
25% quartz and feldspar
3% other minerals
Organic matter <1%
Clays swell, have low permeability, and good ion sorption/exchange capacity
They can play an important role in nuclear waste confinement

## Slide 3
Introduction
Because of the very tiny nature of clay particles (< 2µm), some important phenomena taking place at the aqueous phase – clay interface are difficult to study by experimental methods. And even when available, some experimental data are difficult to interpret.
Computational molecular modeling then appear as complementary powerful tool to facilitate the atomic-scale interpretation of the observed interfacial phenomena, the effects of substrate structure and composition on the structure, dynamics, and composition of the interfacial aqueous solution.
Nuclear waste repository
Optimize our models by building larger, more diverse and realistic clay models.

## Slide 4
Clays are mainly layered phyllosilicates minerals of SiO4 tetrahedral sheets and AlO6 octahedral sheets having various stacking arrangements.
Oxygen
Silicon
Aluminum
Tetrahedral sheet
Octahedral sheet
clay minerals (smectites)
Mg/Al and Al/Si substitutions respectively the in octahedral and/or tetrahedral layers of pyrophillite (Si8)(Al4)O20(OH)4 give rise to montmorillonite. This clay now has a negative layer charge that is compensated by sorption of cations. Ex+y(Si8-xAlx)(Al4-yMgy)O20(OH)4. With y>x and E a compensating cation.
Wyoming montmorillonite: E0.75(Si7.75Al0.25)(Al3.5Mg0.5)O20(OH)4 E = Cs, K
2:1 clays
Pyrophillite (smectite group)
Montmorillonite
Layer charge ~0.75: montmorillonite is a swelling clay

## Slide 5
Pyrophillite atomic structure from X-ray data
Uniform distribution in T and O layers (Uni)
Random distribution in O and T layers (RanTO)
Random distribution in O layers (RanO)
clay minerals (smectites)
Basal oxygen (Ob) : - 1.05 e
Basal oxygen with tetrahedral substitution (Obts) : -1.1688 e
Basal oxygen with octahedral substitution (Obos)
Hydroxyl oxygen with octahedral substitution (Ohs)

## Slide 6
O
H
H
rαβ
θ
Molecular Dynamics: Numerically Solves Newtown’s equation of motion for N interacting particles.
t ~ 1 fs = 10-15 s
Uij = ∑(Aij/rij12 - Bij/rij6 + qiqj /ε0rij) + ∑½kb (rαβ - r0)2 + ∑½kθ (θ - θ0)2
V-d-Waals Coulombic bond stretching angle bending
CLAYFF – specialized semi-empirical fully flexible force field model allowing for realistic exchange of momentum and energy among all atoms – solid substrate and aqueous solution (Cygan et al, 2004).
At time t we know ri(t), vi(t) for all the particles
Molecular modeling is a combination of theoretical methods and computational techniques used to mimic the behavior of atoms and molecules in real natural systems in order to predict their properties.
Molecular dynamics in few words

## Slide 7
Classical Newtonian dynamics
Clay: Wyoming Montmorillonite
E24(Si248Al8)(Al112Mg16)O640(OH)128 E = Cs, K
Ntot ~ 5,000 atoms
NH2O ~ 0-1018 molecules (SPC model)
CLAYFF force field
a  b  c ~ 2  4  2 nm3
Periodic boundary conditions
NPT ensemble T = 298K; P = 1 bar
t = 2 ns (equilibration + equilibrium)
Δt = 1.0 fs = 10-15 s
Basal spacing
Hydration Energy
Immersion Energy
Isosteric heat of adsorption
Simulated systems - 1

## Slide 8
Results and discussions

## Slide 9
Results and discussions

## Slide 10
Classical Newtonian dynamics
E24(Si248Al8)(Al112Mg16)O640(OH)128 E = Cs, K
Ntot < 5,000 atoms
Three first stable hydration states
CLAYFF force field
a  b  c ~ 2  4  2 nm3
Periodic boundary conditions
NVT ensemble T = 298K
t = 1.5 ns (equilibration + equilibrium)
Δt = 1.0 fs = 10-15 s
Simulated systems - 2
Atomic density profile
Radial distribution function

## Slide 11
Uniform
RanO
RanTO
Results and discussions
Water content = 6 H2O / Cs
Atomic density profiles

## Slide 12
Uniform
RanO
RanTO
Atomic density profiles
Results and discussions
Water content = 13,33 H2O / Cs

## Slide 13
Uniform
RanO
RanTO
Atomic density profiles
Results and discussions
Water content = 20 H2O / Cs

## Slide 14
Uni
RanO
RanTO
Results and discussions
Atomic density profiles
Water content = 6,67 H2O / K

## Slide 15
Uni
RanO
RanTO
Results and discussions
Water content = 13,33 H2O / K
Atomic density profiles

## Slide 16
RanO
RanTO
Results and discussions
Water content = 20 H2O / K for RanO and RanTO
= 21,83 H2O / K for Uni
Atomic density profiles

## Slide 17
a
a
b
c
b
a
Radial distribution function
Basal oxygen (Ob)
Basal oxygen with tetrahedral substitution (Obts)
ion – Ob
ion – Obts
ion – Ow
Ow – Ob
Ow – Obts
Ow – Ow
Results and discussions

## Slide 18
Radial Distribution functions
RanO
Uni
RanTO
Results and discussions
Basal oxygen (Ob)
Basal oxygen with tetrahedral substitution (Obts)
Water content = 6,67 H2O / Cs

## Slide 19
RanO
Uni
RanTO
Results and discussions
Radial Distribution functions
Basal oxygen (Ob)
Basal oxygen with tetrahedral substitution (Obts)
Water content = 6,67 H2O / Cs

## Slide 20
Radial Distribution functions
Basal oxygen (Ob)
Basal oxygen with tetrahedral substitution (Obts)
Water content = 6,67 H2O / K
RanO
Uni
RanTO
Results and discussions

## Slide 21
Radial Distribution functions
Basal oxygen (Ob)
Basal oxygen with tetrahedral substitution (Obts)
Water content = 6,67 H2O / K
Results and discussions
RanO
Uni
RanTO

## Slide 22
Conclusions and perspectives
  The next step is to look at the dynamics of the system:
There is no significant difference between the three clay models concerning the studied structural properties.
  Hydrogen bonding network
  Diffusion coefficient of aqueous species
The same studies are being carried out for a series of other cations ( Sr2+, Ni2+)
The " Uniform " clay model shows a lower hydration energy compared to the two other models for both Cs and K.
The hydration energetics indicate that in addition to the commonly observed 1-layer and 2-layer hydrates, stable hydration states corresponding to 3-layer and 4-layer hydrates can also be distinguished.

## Slide 23
Acknowledgments
These work is being carried out in the context of the industrial chair «Storage and Disposal of Radioactive Waste» at the Ecole des Mines and thanks to
CURIE,TITANE, Partnership for Advanced Computing in Europe (PRACE), at CEA, Bruyères-Le-Châtel, France
CINECA computing center (Italy)
JADE, Centre Informatique National de l’Enseignement Supérieur(CINES), Montpellier, France
We are also grateful for computer time allocations :
Prof. Andrey Kalinichev
Dr. Narashimhan Loganathan
Many thanks to :
Dr. Julie Champion
Thank you for your kind attention