## Slide 1: SMART PIXELS and 3D APPROACH
P.Pangaud
CPPM

## Slide 2: Tezzaron-Chartered technology
Main characteristics :
2 wafers (tier 1 and tier 2) are stacked face to face with Cu-Cu thermo-compression bonding
Via Middle technology : Super-Contacts (Through Silicon contacts) are formed before the BEOL of Chartered technology.
Wafer is thinned to access Super-Contacts
Chartered technology limited to 5 metal levels
Back-side metal for bonding (after thinning)
One tier
Bond interface layout
Wafer to wafer bonding

## Slide 3: Access to the TC technology
Global Foundries (Chartered) 0.13µm LP and Tezzaron technologies
  Semi-annual MPW runs via CMP-CMC- MOSIS: 2,000 $ /mm²
      Example 2.5 mm x 2.5 mm = 12,500 $
  Dedicated run with TEZZARON : ~350,000 $ for 1 masks set
The CMP-CMC- MOSIS price is acceptable for a chip smaller than a block size
The maximum block/prototype size is
12.69mm x 15.19mm.
Can we reach a custom 12.69mm x 20 mm prototype size?

## Slide 4: TSV and Bond Interface
The TSV are realized after the FEOL stage and before the BEOL stage (diam of 1,2µm)
The bond Interface are mechanical and electrical interfaces to connect 2 tiers together by face to face Cu-Cu thermo-compression.
Tezzaron uses the 1µm thick Cu TopMetal to create the “leopard skin”.

## Slide 5: HV technologies
  Best Case
  0,13µm HV Global Foundries is an option of 0,13µm LP technology
0,13µm LP -> Tezzaron
0,13µm HV -> Tezzaron ???
Substrate Resistivity = 20 ohm.cm
If -32V, depleted depth = 7,3µm
Can we design LV Tr into HV_NWELL?
Can we use DNWELL with substrate at -32V?
We are waiting more information
1µm thick Cu TopMetal

## Slide 6: HV technologies
  Other solution
  0,18µm HV Global Foundries
Substrate Resistivity = 20 ohm.cm
If -32V, depleted depth = 7,3µm
Can we design LV Tr into DVNWELL?
Can we use DVNWELL with substrate at -32V?
We are waiting more news
1µm thick Cu TopMetal
The BuriedPP and DVNWELL layers also exist for the 0,13µmHV GF technology, but they are optional.
Awaiting more news
0,18µm HV -> Tezzaron ???

## Slide 7: HV technologies
  Other solution
  0,18µm HV AMS
4µm thick Cu TopMetal
Substrate Resistivity = 10 ohm.cm
If -50V, depleted depth = 6,7µm
0,18µm HV -> Tezzaron ???

## Slide 8: Depleted parameters from models

## Slide 9: smart pixels schedule – prototypes for 3DIT
Can we design a smart pixel by using the Tezzaron-Chartered 0,13 LP technology?
  We need more news from the GlobalFoundries
    A loooooooooooong way….
What about the GF 0,18µm HV technology?
canceled

## Slide 10: 3D smart pixels schedule
Tezzaron-Chartered 0.13µm LP technology schedule
  Semi-annual run (March and October)
  If the GF 0.13µm HV is relevant, can we use the 0,13µmLP technology and adding HV masks? How many masks? Price?
    Awaiting answers
  If the 0,18µm HV (GF or AMS) are more relevant, can we 3D-connect them with an other tier (GF 0,13µm LP ; GF 65nm ; TSMC…)? Tezzaron be able to realize it? The High thickness of AMS TopMetal is a problem? Price? Etc ….
    This is being discussed with Tezzaron….