## Slide 1: A_RD_9 Effort towards improving large scale production of SC cavities

## Slide 2: Members for A_RD_9

## Slide 3: Outline
Context and motivation for our proposal
New equipment at CEA/Irfu : Vertical Electro-Polishing (VEP) set-up
New equipment at KEK: Cavity Fabrication Facility (CFF)
New process
  Optimized Electron Beam Welding (EBW)
  Electro-Chemical Buffing (ECB)
  Modified VEP process by Marui Company
  Details of the program
  Summary

## Slide 4: Context: SCRF Industrialization required for ILC
Parameters | Value
C.M. Energy | 500 GeV
Peak luminosity | 1.5 x1034 cm-2s-1
Beam Rep. rate | 5 Hz
Pulse duration | 0.73 ms
Average current | 5.8 mA (in pulse)
Av. field gradient | 31.5 MV/m +/-20% Q0 = 1E10
# 9-cell cavity | 16,024 (x 1.1)
# cryomodule | 1,855
# Klystron | ~400
16024 x 1.1(Yield = 90%)
~ 17600 cavities of mass-production
High quality
Linac (11km) x 2
ILC

## Slide 5: Progress in SCRF Cavity Gradient
Production yield:
94 % at > 28 MV/m,
Average gradient:
37.1 MV/m
reached (2012)
Issues of mass-production:
High Quality Assurance (QA)
Cost Reduction

## Slide 6: Motivation
Previous collaboration within A_RD_5 program: Surface treatment
>>> Very successful
We installed new equipments at KEK & Irfu.
  Extension of our expertise from cavity fabrication to Vertical Test.
  Equipments of KEK & Irfu are complimentary and this collaboration makes us the efficient R&D possible.
  The collaboration between KEK & Irfu will play the important role to establish the cavity mass-production of ILC.

## Slide 7
reception
Eddy-current
scan
Press forming
Trimming
Inspection
CP
stock
EBW
EBW
Bulk EP
anneal
Inspection
Tuning machine
Jacket
Stock area
AC power area
Assuming area（53m x 30m）
Simulation study of cavity production plant
KEK-MHI
Assuming that final treatment and vertical test will be done in other place.
parts delivery
Cavity fabrication and cavity surface treatment are the most important parts of ILC mass-production.
surface treatment
R&D at CEA Saclay/ Irfu
Fabrication / R&D at KEK

## Slide 8
Vertical Electro-Polishing
(VEP) Set-up at CEA Saclay

## Slide 9: Horizontally Rotated Electro-Polishing (EP) - Conventional
Cavity X-section
Beam Pipe
Cathode
Cathode
bag
Acid
Level
EP acid
circulates
Circulating EP acid
H2SO4(95%) : HF(46%)
= 10 : 1 in volume
Electric
Current
Voltage ~ 20 V, Current ~ 40A
Back to EP-acid
reservoir
tank (100L)
2
Temperature
sensor

## Slide 10
9-cell horizontal EP setup (KEK): electrolyte is half-filled
9-cell vertical EP setup (Ifru): electrolyte is fully filled.
Horizontal vs Vertical

## Slide 11
Overview
VEP of 1Cell and 9-cell cavities
Focus on parameters: low voltage (~ 6V) – high acid flow (25L/min)
  Improved degassing (H2 , O2)
  Lower heating
Four 1-Cell cavities and one 9-cell cavity were prepared by VEP
TB9RI025 cavity
Prior to VEP
Circulating acid
Constant voltage
Nitrogen blowing

## Slide 12: Horizontal vs Vertical
Pros:
Good evacuation of gases (cavity half filled)
Demonstrated performance
Large range of parameters
Cons:
Complicated process (high cost)
Rotary seals
Switching (vertical draining) of the cavity
Low removal rate (half-filled)
Pros:
Simple process (low cost)
Improved safety
Higher removal rate (Fully filled)
Cons:
Sensitive to fluid dynamics
Difficult evacuation of gasses
Proper parameters to be determined…
…Voltage and fluid velocity

## Slide 13: Low Voltage VEP: 1st Result
Better surface achieved
Pits partially removed
In spite of pits, the cavity is tested
→ Quench at 34MV/m at the pit area
(Standard Q-Slope before baking)
VEP of cavity with low surface quality (pits)
ILC specification of Eacc at VT: 35 MV/m

## Slide 14
Eacc > 41 MV/m on 1Cell Cavity with Parameters:
Low Voltage – High Acid Flow
1DE1: Horizontal EP + 70 µm VEP
Parameters: 6V & >24L/min
Bright and smooth surface
Performance before/after baking similar to HEP
High gradient maintained after VEP
1DE1 after HEP + 70 µm VEP
Aspects to improve:
Low removal rate at 19°C: 0.2µm/min
asymmetry: removal rate higher in the upper part of the cell (x 3)
Acid flow
higher local removal
ILC spec.

## Slide 15
Cavity Fabrication Facility
CFF at KEK

## Slide 16: Construction of Cavity Fabrication Facility (CFF)
STF building
Map of KEK
Chemical treatment
Surface inspection
Vertical lathe
Press machine
EBW
Clean room 19m x 14m x 5m
Clean room floor layout of CFF
Cavity Fabrication Facility
(CFF)
Construction finished in FY2011
All machines are in class-100,000 clean-rooms.

## Slide 17
Main Equipments of CFF
Inspection equipment for Nb surface
EBW room
Installation of EBW machine started from April 2011.
Vertical lathe
Press machine (servo control)
Measuring system for half cell shape (Under developing)
Chemical Polishing room

## Slide 18
Purpose of Cavity Fabrication Facility (CFF)
High performance / high yield rate = Good QA
Reduction of fabrication cost
R&D of mass-production processes/fixtures
All necessary machines for cavity-fabrication are in one place: Efficient R&D
Studies in CFF
Cooperation with vendors (industries)
Cooperation with STF (Surface treatments / VT in Lab.)
Speed up the R&D to establish the standard recipe for mass-production
Open to other lab. / venders
Target is realization of mass-production technology for 17,000 cavities (ILC).

## Slide 19: Plan/Purpose of cavities in CFF/KEK
FY2012
FY2013
fabrication
VT
KEK01
fabrication
VT
KEK02
fabrication
VT
Jacket weld
KEK03
Preparation for complying with high pressure gas code
Demonstration of mass-production
Cavity
KEK00
VT
Jacket weld training
Cryomodule-1
8 cavities
CM2a
4 cavities
CM2b
4 cavities
KEK-03 cavity (Fabrication in CFF/KEK)
STF/KEK
We are here

## Slide 20
Improvement of EBW Process at KEK

## Slide 21: Fabrication of KEK-01 Cavity with HOM

## Slide 22
Configuration Choice of Cavity Attitude and Gun Position
Direction of electron beam is vertical.
Stacking dumbbells is easy in the vertical configuration of cavity.
Better for mass-production.
Setting cavity in horizontal way is rather compllicated (KEK-00).
Direction of gravity.
Direction of electron beam is horizontal.
Setting cavity in vertical way is simple (KEK-01).

## Slide 23
EBW at equator for stacked dumbbells (KEK-01)
Direction of electron beam
Direction of electron beam
Direction of electron beam
EBW test by a dummy Nb-pipe
Rotation
Beam current (mA)
Rotation angle (degree)
Overlap
Parameter for equator
EBW of 2-dumbbell
EBW of 4-dumbbell
Smooth inner surface of welding seam was achieved.
120 kV, 5 mm/s

## Slide 24: Design of loader for multiple dumb-bells
e- gun
on side
Pumping time (~30 min.) and cooling time (~30 min.) are duplicated in EBW processes.
Multiple dumbbells are loaded inside the EBW chamber at once and the EBW of dumbbells will be done continuously after pumping down.
Proto-type of four-dumbbell loader

## Slide 25
New Processes Investigated

## Slide 26
● A rotating disk with abrasive fine particles on nonwoven fabric is pressed against the workpiece.
● An aqueous solution of sodium nitrate (neutral) is supplied in between.
● The disk and the work function as a cathode and an anode, respectively.
● Abrasive : micropowders of alumina, diamond, silica etc.
● Current : a few of mA/cm to a few of 10mA/cm2 depending on the polishing stages.
Electro-Chemical Buffing (ECB) by KEK

## Slide 27
Smooth Surface on Dumbbells
ECB makes it possible to achieve very bright surfaces on dumbbells

## Slide 28
Rq=0.39μm
Rq=0.04μm
ECB
EP
1mm
1μm
Decreased Roughness

## Slide 29
New VEP Method by Marui Company Ltd

## Slide 30
To remove hydrogen gas generated during EP process by the method of fluid circulation.
A part of features : Integrated New VEP System
New VEP Process with top-down Electrolyte Circulation by Marui Cy Ltd
Flow direction
Acid bath
Pump
Flaws observed after VEP with inadequate parameters (voltage, Temp, Cathode shape):
stripes (due to bubbles)
Pitting
This new method should overcome these pbms

## Slide 31
Details of the Program

## Slide 32
Manufacturing of New 1Cell Cavities
Dedicated to ECB
Two single-cell cavities have been fabricated for ECB experiments:
Tesla shape: K-LBW-S01-ECB
Low Loss shape: 1TS-01-ECB
These cavities will be ECB’ed at KEK and shipped to Irfu for Assembly and VT.

## Slide 33
Next Step Plan at Marui – VEP on Nb. Cavity
1-Cell TI00 Cavity purchased from RI company
  VEP at Marui + VT at Saclay
Cavity Exchange program between Marui and CEA.
  TI00 Cavity VEP’ed at Marui, Vertical Test (VT) at Irfu
  1AC3 VEP’ed at Saclay (36MV/m) will be shipped to Japan for VEP
  VT at Irfu
  →Comparison of respective results at Marui / Irfu
If successful results, motivation for 9-cell VEP at Marui & Irfu
MG purchased from RI GmbH
Inside the 1-Cell Cavity

## Slide 34
Summary
Previous collaboration within A_RD_5 program was very successful.
New equipments are installed at KEK & Irfu.
Cavity Fabrication Facility (CFF) at KEK
Vertical Test Facility at Irfu.
  Extension of our expertise from cavity fabrication to Vertical Test will realize more effective R&D of ILC mass-production process.
  Equipments of KEK & Irfu are complimentary and this collaboration makes us the efficient R&D possible.
  Detailed cavity-exchange plan are considered.
  The collaboration between KEK & Irfu will play the important role to establish the cavity mass-production of ILC.

## Slide 35
Backup slides

## Slide 36: Studies on EBW parameters
Search for good EBW parameters was done by changing the welding beam-voltage, beam-current, focus-current, working-piece distance from gun, working-piece moving speed, Nb-plate thickness, and the gun and working-piece configuration.
Horizontal beam
Downward welding
Horizontal beam
Upward welding
In particular, the gun and working-piece configuration affects the results of welding seam.
Vertical beam
Horizontal beam
(See next slide)

## Slide 37
Local grinding at KEK
~115µm depth pit in MHI-08 cavity
Grinding only for pit, without touching other surface
diamond powder compound
with water in between
were used.
MHI-08 cell #2 grinding example
This pit caused quench at 16 MV/m
Quench at 16 MV/m