## Slide 1: 3D Detector Simulation with Synopsys TCAD
V. Gkougkousis1,2, A. Lounis1,2, N. Dinu1, A. Bassalat1,3
Journée de la simulation 17/6/2013
Laboratoire de L'accélérateur Linéaire
Université Paris-SUD XI
CERN

## Slide 2: Outline
Introduction
  Past advances and future intentions
  The tool: Status and capabilities
Genic simulation principals
  General Process Flow
  Optimization strategies
  Implantation models
Concrete cases
  Test Diode example
  2D IBL single pixel simulation
  Full 3D IBL single and multiple pixel geometries
  Edgeless Detectors Status
Dopant profile measurements
Conclusions and plans

## Slide 3: Introduction & Status
Passing to 3D Simulations
Migrating from SILVACO TCAD to Synopsys
Both process simulation and irradiation model integration
Tools
Radiated IBL structures simulation
Charge sharing and electrical field distributions
Defects modeling and model testing
Validate Edgeless VTT geometry and radiation hardness
Geometry and fabrication process flow simulation
Detailed investigation of electrical field on detector edge
Charge propagation in the substrate and boundary conditions effects
Radiation hardness modeling and simulation
Intentions
1 Guard Ring
Guard Ring + Bias Rail
No Guard Ring or Bias Rail
IBL Voltage simulation (600V - 5 x1015neqcm-2)

## Slide 4: Introduction & Status
Technical support can be an issue
Central Licensing management plus bush capabilities essential
License
  One available license with minimum parallelization
  Three on-line license servers required
  Managed by LAL, accessible only via intranet
  No batch possibility at the moment (lxplus / ccage have no access to licenses)
  Multiple instances can be used, up to two per tool
  No multithreading support
Status
Portable Linux-based installation
Out-of-the-box functionality
No software dependences
Memory and CPU consuming

## Slide 5: Generic Principals
Create a fabrication process flow to simulate geometry
Associate with corresponding mask directly from GDS files (usually provided)
Introduce the required parameters (dose, energy, implantations)
Set-up an appropriate meshing strategy for the desired application
Set up required re-meshing along the process to speed up simulation
Introduce variables and create multiple experiments
Preview strictures and profiles, feed-in parameters to other tools
+
-
No need for detailed geometry definition
Graphical interphase for speed with command functionality
Comprehensive simulation
Detailed process flow never known
Re-meshing mandatory in each geometry change
Optimized for small scale devices and interface simulation between different materials

## Slide 6: Optimising…
The Mesh
  Define meshing strategy adapted to the specific geometry with finer cell size in transition regions
  Initial mesh valid until geometry change (first deposition, each), define re-meshing strategy before
  Avoid thick photosensitive layers since they are even meshed after stripping
  Usually simulate fist few microns of substrate wafer and add full silicon thickness at the end
  In bilateral processes each flip causes geometry redefinition (no true bilateral integrated)
The model
  MC simulation or numerical solution to diffusion differential equations
  Number of particles to be simulated and extrapolate
  Physical model to be used

## Slide 7: Optimizing….
The refinements
  Implants energy and dose relative and absolute error
  Desired accuracy in concentration determination and profiles
  Grid refinements in transition regions (necessary to calculate solutions in dopants)
  Request multiprocessing
  Implantation Model
  Analytic implantation: simple Gaussian/Pearson and dual Pearson functions, based on spatial distribution of ions described by moments depending on species, energy e.c.t. Numerical values given by tables
  Monte Carlo method atomistic simulation of ion implantation with Sentaurus MC, or Crystal-TRIM originated from the Transport of Ions in Matter (TRIM) code. Simulates ion implantation into single-crystalline materials or amorphous materials of arbitrary composition

## Slide 8: Concrete Cases: Test Diode
Simple geometry
Known dopant profiles
Large structure
Experimental iv curves to compere with simulation
Simulation fails!!!!!
Pros: Simple geometry that allows model testing with simulated process flow No Backside structure
Conns: Very large structure, enormous mesh with numerous cells which depletes available memory (in all platforms)
Dimensions 3000 x 3000 μm
No Nitride layer – p-spray

## Slide 9: Concrete Cases: IBL 2D
Simulation Succeeds!!!!!
Complete pixel geometry
Have to start from basic parameters (dopant profiles not exactly known)
Small structure
Experimental iv curves to compere with simulation
Pros: Complicated geometry with multiple layers Backside processing present Have to do front and back side separately and merge results Small size so limited number of grid cells
Conns: Aspects that are not yet completely understood in geometry file 24 hours for first imlantation
Dimensions 250μm wafer thickness x80x25 Complete implantation

## Slide 10: Concrete Cases: IBL 2D
Finer meshing in transition region
Phosphorus profile
N profile in 2D IBL pixel simulation on the punch through side.
Wafer is N with concentration of 1011 in the bulk. A thin 30nm Oxide layer remains.
Transition region between Si – Oxide layer
Adaptive meshing in transition regions

## Slide 11: Concrete Cases: IBL 2D
Geometry
Phosphorus profile
Meshing of the photosensitive region
Images of the same region of the pixel in the punch through side.
Dimension ration distorted to display surface structures
All 250 μm of the wafer are simulated
Photoresist is present in the upper left plot

## Slide 12: Concrete Cases: IBL 3D
Complete 3D double sided pixel geometry
Use basic parameters (dopant profiles not exactly known)
Full depth substrate simulation
Time of full single pixel run ~ 6h
Bilateral process flow
Process flow with ~50 stages
3 Pixel geometry also available
Carried out with one energy and dose but several scenarios are available

## Slide 13: Concrete Cases: IBL 3D
Geometry
Meshing strategy
N implant
P implant
Detail of the p-Spray region between the pixels showing meshing, geometry and implants concentration

## Slide 14: Concrete Cases: IBL 3D
Finer Meshing in the Guard Rings

## Slide 15: Default Parameters
Silicon Substrate
  Type: n, Phosphorus doped
  Orientation: 100
  Resistivity 5000Ohm/cm3
  Thickness: 250μm (actual depth for simulation 5μm)
Oxide Layer
  Isotropic deposition of 150nm
  Anisotropic etching with a remaining 20nm layer
Photoresist
  2μm isotropic deposition followed by strip etching after development
n Implant
  Phosphorus at 60keV, dose of 1015 particles/cm2 with angle of -900

## Slide 16: Default Parameters
P Spray
  Boron at 100keV, dose of 1013 particles/cm2 with angle of -900
Annealing
  300 minutes at 900 C, pressure of 1atm (literature reference of 3 temperature zones and pressures in the order of 500torr)
Metallization - Passivation
  Aluminum contacts formation from isotropic CVD deposit
  SiO2 passivation layer for mechanical and electrical protection (no implication in simulation result)

## Slide 17: Process Flow Complexity
IBL
55 separated steps, various variables and 8 macros
30 steps with 5 macros, no back processing
Diode

## Slide 18: Edgeless Detectors
GDS Files have been provided
Not complete understuding of the fabrication process
Scribe cleaning passivation poses simulation problem
Several efforts are in the way
Contacts in the near future with the industry (hoping to get input and details)
To Do, Effort on the way

## Slide 19: Conclusions and plans
Goal to simulate edgeless detectors
likelihood approach for doping profiles to define correct parameters
Support a central licensing management which would allow multiple instances and parallelization
Compare simulation results with experimental measurement in dopant profiles, charge shearing
Simulate irradiated detectors and describe their behavior in the effort for radiation hardness
Explore alternative geometries for bias rail / bias dot / guard ring structures

## Slide 20: Backup

## Slide 21
Dopants profiles - SiMS
SIMS system @ CNRS-Meudon (Cameca IMS 4F)
  Analytical technique to characterize the impurities in the surface and near surface (~30m) region
  Relies on sputtering of a primary energetic ion beam (0.5-20 keV) on sample surface and analysis of produced ionized secondary particles by mass spectrometry
  Good detection sensitivity for many elements: it can detect dopant densities as low as 1014 cm-3
  Allows multielement detection, has a depth resolution of 1 to 5 nm and can give a lateral surface characterization on a scale of several microns
  Destructive method, since the act of the removing material by sputtering leaves a crater in a sample
  It determines the total dopant density profile
Easily accessible

## Slide 22
Pair of specially conditioned point contact probes which are stepped across the bevel surface of the semiconductor sample
Resistance between two probes is measured at each step
Resulting data computer processed into detailed carrier concentration and resistivity profiles from which dopant concentration profiles can be deduced
Dopants profiles – SRP
Costly Technic carried out by Evans Analytical Group
No full control of used parameters
Development of in-house alternatives
Analytical technique to characterize the majority carrier and active dopant concentration profiles in semiconductor structures
Pros: Very high dynamic range (1012 – 1021 cm-3) Capable of profiling very shallow junctions (nm regime)
Conns: Destructive method
Procedure

## Slide 23
Dopants profiles
n+/n
p+/n
Measurements on n-on –n wafers
Good overall SiMS SRP agreement
Not all implanted dopant atoms are integrated in lattice positions, not all electrically active
N+ implant characteristics
  SIMS peak conc. Nn ~ 1x1019 cm-3
SRP peak conc. Nn ~ 8x1018 cm-3
P+ implant characteristics
  SIMS peak conc. Np ~ 3x1019 cm-3
  SRP peak conc. Np ~ 5x1018 cm-3