## Slide 1
SRF2013 TUTORIAL
BASIC PRINCIPLES OF RF SUPERCONDUCTIVITY
Enzo Palmieri
ISTITUTO NAZIONALE DI FISICA NUCLEARE
Legnaro National Laboratories
and
University of Padua
ITALY

## Slide 2
Let us build a resonant cavity

## Slide 6
E ~ E0 eiwt
E0  B0  E0 + E1  B0 + B1  E0 + E1 +E2 

## Slide 10
By Radiofrequency one can accelerate particles to high energy without the need of the equivalent high static fields

## Slide 11
Chain of weakly coupled pill-box cavities representing an accelerator module

## Slide 12
Coupled pendula for a mechanical analogous
Zero mode
p-mode
There are N eigen-modes for such an oscillating system
The smallest RF losses

## Slide 13
  A normal metal exposed to RF fields

## Slide 14
Normal metals in RadioFrequency and the normal skin effect
Normal metal
Vacuum
Ey(0)
d
k = k1 + i k2

## Slide 15
For a semi-infinite conductor filling the +x half-space and has a plane surface at x = 0
THE ELECTROMAGNETIC RESPONSE OF A METAL
z
y
x
metal
Vacuum
H
E

## Slide 16
THE ELECTROMAGNETIC RESPONSE OF A METAL

## Slide 17
z
y
x
metal
Vacuum
H
E

## Slide 18
w ; T
d
J(r) = s E(r)

## Slide 19
:
The Anomalous Skin Effect

## Slide 20
The Two fluid Approach for describing the phenomenology of a Superconductor

## Slide 22
Two Fluid model for a superconductor
Electrical Conduction mechanism due to 2 different components
Normal
Superfluid
TC T
1
nS/n
nn/n
J = Jn + JS

## Slide 23
J = Jn + JS
Jn = s E
JS = ns e vs
m vs = -e E
London equation
Is the Analogous of the
“Ohm Law” for Superconductors

## Slide 24
Superconductors
I type
II type
Pippard
London
The l dependence vs mfp induced Pippard to modify London’s model
He borrowed from Chambers the non local approach that relates Current and Electric field

## Slide 25
Strong Correlations among Superelectrons
within a coherence length x0
instead of
xo
l
xo
l
London
Pippard

## Slide 26
xo
l
xo
l
London
Pippard
Pippard x > l
London x < l
x = x0 if l∞
otherwise
If l then
x
l

## Slide 29
J. Bardeen L. Cooper R.Schrieffer
Cooper Principle:
Between 2 electrons excited above Fermi Energy, it exists a pair bound state separated by D from EF, however weak an attractive interaction is supposed

## Slide 31
c

## Slide 32
The Surface Resistance for a Superconductor: BCS contribution

## Slide 33
The power losses through the walls of a resonator
may be described by the quality factor Q
V is the volume enclosed by the resonator,
A is the resonator surface and w is the resonance frequency
In the approximation of an uniform magnetic field on the surface
where G is a geometrical factor equal to 254 W for the TESLA type shape.

## Slide 34
R is the real part of a complex quantity, the surface impedance
Z = R + i X
the surface resistance R measures dissipation processes of rf fields into the medium surface,
the surface reactance X measures the phase shift of a wave upon reflection from the surface.

## Slide 35
The results for normal metals can be easily extended to superconductors, when a complex conductivity s1 - i s2 is introduced in place of the normal state conductivity sn.
Hence, as derived by Nam
where m = - 1/3 for the Pippard limit,
and m = - 1/2 for the London limit
Rs can be so written as

## Slide 36
in the London limit to
However when s1 << s2, (T < Tc / 2), this relation simplifies to

## Slide 37: In the two fluid approximation
where

## Slide 38
J = Jn + JS
T =TC; w ≠ 0  RS ≠ 0

## Slide 39
seff = s1 – js2 ≈ sn (nn/n) – j (1/wm0l2)

## Slide 40
The MB expressions were found also valid in the limit of impure superconductors by Nam.
The two integrals s1/sn and s2/sn are easily numerically calculated. In particular they can be approximated in the normal skin effect regime for h'w << 2 D and w2 t << 1 (t is the momentum relaxation time) by:

## Slide 43
s1-is2 in place of sn
Surface Impedance and Surface Resistance
For a normal metal in the normal regime:
sn = 1 / rn = dc conductivity at T
d = skin depth
As derived by Nam, for T < Tc / 2, Rs can be approximated by:
Extension to Superconductors:

## Slide 44
In the framework of the BCS theory, for w < 2 D, the complex conductivity of a superconductor is:
Mattis and Bardeen Integrals
in the extremely anomalous
The second integral in s1 / sn does not appear unless w > 2 D.
In such a case the lower limit of the integral in s2 / sn is - D instead of D - h'w.

## Slide 45
and
D ( T ) = D (0) . { cos [ p ( T / Tc )2 / 2 ] }1/2

## Slide 46
Mattis and Bardeen Integrals
The two integrals s1/sn and s2/sn are easily numerically calculated.
In the normal skin effect regime, for ħw << 2 D

## Slide 47
since the effective penetration depth l,
related in the London limit (x3 << x0 lL 2),
to the classical London penetration depth lL by
or

## Slide 48
RBCS
Then, if T < Tc / 2
where A = 6.0 E-21

## Slide 49
RBCS
Then,
(Empirically, Rres is found to be dependent on rn too)

## Slide 50
For low rf losses,
a high TC value is not sufficient
A metallic behaviour
in the normal state is mandatory
Essence of the previous calculations

## Slide 51
T= 4.2K, f = 500MHz, S=4
After C. Benvenuti, V. Palmieri, R. Vaglio, "Construction Materials for Superconducting RF accelerating cavities", P. Vincenzini ed., Advances in Science and technology 8, Superconductivity and Superconducting Materials Technologies, Techna publ. Faenza (1995), pp. 637-648.

## Slide 52
c
Or equivalently

## Slide 53
The validity of previus formulas is however limited to the dirty limit superconductors, but Niobium fails out of this limit, when l becomes comparable with x0 : in such a case RBCS even increases when the Niobium purity is enhanced.
Although our approximation is valid only in the dirty limit, we asssume to not committ a large error if such relation is analitically prolongated in the London limit.

## Slide 54
In this case the penetration depth l becomes

## Slide 55
B is the Nb RRR values one obtains

## Slide 57
the formula has a minimum for values of b around 10

## Slide 60
The field dependence
of BCS contribution

## Slide 61
For any chemical reaction, there must be a minimum amount of energy between reactant molecules for effective collisions between them. This is termed as activation energy.
Modified Arrhenius Equation

## Slide 63
At room temperature, most of the molecules have less than the threshold value. Hence, if energy is supplied to the reactant molecules in the form of light or heat, they absorb that energy and reach a higher energy level which is equal to or greater than the threshold energy level.
Modified Arrhenius Equation

## Slide 64
Modified Arrhenius Equation
Activation energy (Ea) = Threshold energy - Average kinetic energy of molecules Those reactions which have less magnitude of activation energy (Ea) are completed fast while some reactions appear to be slow due to higher activation energy

## Slide 65
Activation energy (Ea) = Threshold energy - - Average kinetic energy
D = D0 - Ks

## Slide 67
?
D = D0 - pfvs
I.I. Kulik, V. Palmieri, "THEORY OF DEGRADATION AND NON LINEAR EFFECTS IN Nb-COATED SUPERCONDUCTING CAVITIES",
Proceedings of the Eight Workshop on RF Supercoductivity, Abano, Italy, October 1997, V. Palmieri, A. Lombardi eds.
Special Issue of Particle Accelerators, Vol. 60,(1998)p.257-264
The Ginzburg-Landau result
D= D0 (1 – H2/HC2)
does not apply!!!

## Slide 68
D= D0 (1 – H2/HC2)
This formula has done a lot of damage to our community for the understanding of the Q-Slope
R.H. White and M. Tinkham, Magnetic-Field Dependence of Microwave Absorbtion and Energy gap in Superconducting Films, Phys Rev, vol 136, 1A, (1964), p. A203
“…..The qualitative features of D/D0 dependences like (1 – h2) and (1-h2)1/2 arevery different from those of the experimental absorption curves reported here …. due to the disagreement between these results and previous theory and experiment, it must be concluded that the above procedure for determining an effective energy gap parameter as a function of H is too naive.”
Y. Nambu, S.F. Tuan, Phys, Rev. Lett. 11, 119 (1963); Phys.Rev.133, A1, (1964)
“…Electrons moving parallel to the surface play a special role: since the magnetic filed will confine such an electron and the one with which it is paired to opposite surfaces of the film, they contribute little to the superconductivity pairing energy…”

## Slide 69
D = D0 - pfvs
It means to take into account the supercurrent!
If for Superconducting Magnets the fundamental and indipendent parameters are 3: TC, HC and JC, …..
This relation goes back to first principles

## Slide 70
Why for Superconducting cavities, JC disappeared?
Is 40 MV/m (1600 G) a field not strong enough?

## Slide 71
REVIEWS OF MODERN PHYSICS VOLUME 34, NUMBER 4 OCTOBER 1962
Critical Fields and Currents in Superconductors*
JOHN BARDEEN
UNIVERSITY OF ILLINOIS, Urbana, Illinois
… II.THERMODYNAMIC RELATIONS
To discuss the thermodynamics of a superconductor in a magnetic field or with current flow, it is most convenient to take the external field H and the superfluid velocity vs as independent variables. ……
The displacement of the pairs causes an increase in free energy of the system which may be expressed simply in terms of Js……
APPENDIX B. DIRECT CALCULATION OF CHANGE OF GAP WITH CURRENT
... In the low temperature limit, there are no excitations formed and thus no change in D until the velocity vs reaches the value for which it is favorable to form pairs of excitations, corresponding to transfer of an electron from one side of the Fermi sea to the other.This criterion is (depairing condition)
or

## Slide 78
The parasitic term PfVs is neglectable at high value of the pure bulk Nb case
It becomes important at low
- thin film case
- contaminated surface after low temp baking

## Slide 79
D = D0 - pfvs
This will affect l0 and Bc

## Slide 80
Courtesy C. Benvenuti et al
Is a key parameter; low values give:
- high Q
- higher slope
For film coated cavities there is no hope to get rid of the slope, unless RRR is increased, but in this case Q values will be lower than the actual

## Slide 81
2 K
1,8 K
1,6 K
Q
0
High field Q-drop
0
10
20
30
40
E
acc
[MV/m]
10
11
10
9
10
10

## Slide 82
In local electrodynamics of superconductivity, j = j1+j2
Where J1 is the Meissner current
At small supercurrent
but at larger Vs, GL theory foresees a deparing effect by the current
Vs
Vs
Vs
D
ns
Js
Vm
Over Vm the superconducting state become unstable

## Slide 83
The low field Q slope

## Slide 84
Questions:
Is the low-field Q-slope a calibration problem?
If not, which is its physical reason?
and in such a case…..
0
10
20
30
40
E
acc
[MV/m]
10
Q
0
1,6 K
10
11
9
10
10
Is something pulling up the Q ?
The Q is originally higher, but for some reason at low field, it decays?
(if understood, it could be beneficial)

## Slide 85
Courtesy C. Benvenuti et al
Nb/Cu sputtered cavity at CERN
Before Abano/Santa fè Workshops (1997/1999):
the low field Q-slope was reported only for Nb/Cu cavities
Since first cavities were baked in the cryostat at ~150°C for ~48 hours
the low field Q-slope was also reported for bulk Nb cavities

## Slide 86
Cavity spun at LNL and treated/measured at KEK

## Slide 87
(Courtesy G. Bisoffi)

## Slide 89
Typical plot of Qo vs Eacc for cavities treated by Dry Oxidation of the surface after a medium temperature annealing
Renzo Parodi - RF SUPERCONDUCTIVITY AT INFN_GENOA
Presented at the 9-th RF Superconductivity Workshop, Santa Fè, NM, 1999

## Slide 90
SC 1
SC 2
a
l1
l2
Vacuum
Hz
Let us suppose that:
on bulk niobium (SC 2 ) we put an overlayer of a different superconductor (SC 1)
a is the tickness of the SC 1
l1 is the penetration depth of the SC 1
l2 is the penetration depth of the SC 2

## Slide 91
Two Superconductors:
SC 2 + SC 1
SC 1
SC 2
a
l1
l2
Vacuum
Hz

## Slide 92
SC 1
SC 2
a
l1
l2
Vacuum
Hz

## Slide 93
SC 1
SC 2
a
l1
l2
Vacuum
Hz
For a “2 Superconductor system”
l1/a
Q2
Q1
DQ

## Slide 94
Medium field Q-Slope
0
10
20
30
40
E
acc
[MV/m]
Q
0
2 K
1,8 K
1,6 K
10
11
10
9
10
10

## Slide 95
SC 1
SC 2
a
l1
l2
Vacuum
Hz
Q2
Q1
l1/a
An hypotesis:
Gap and Penetration depth depends on magnetic field

## Slide 96
SC 1
SC 2
a
l1
l2
Vacuum
Hz
Q2
Q1
l1/a
Q2
Q1
l1/a