## Slide 1
Dr. David Flores
Instituto de Microelectrónica de Barcelona (IMB-CNM-CSIC)
Barcelona, Spain
david.flores@imb-cnm.csic.es
Simulation of Radiation Effects
on Semiconductors
Design of Low Gain Avalanche Detectors

## Slide 2
Outline
General Considerations
  Background
  Basic principles
Ionization Damage Simulation
  Silicon
  Silicon oxide
Displacement Damage Simulation
  Semiconductor
Case Study: Design of Low Gain Avalanche Photodetectors
  LGAD structure and application
  Gain simulation
  Design of active region
  Design of periphery and edge termination region
  Fabrication and Experimental results

## Slide 3
General Considerations

## Slide 4
Centro Nacional de Microelectrónica

## Slide 5
IMB-CNM Main Pillars & R&D Activity
R&D
Training
Technology Transfer
Semiconductor Devices
Power Devices
Integrated Circuits and Systems
Sensors, Actuators and MEMS
Nanoscale Devices and Actuators
Lab-on a chip, Polymer devices
Centro Nacional de Microelectrónica

## Slide 6
  Main CR
  1,500 m2
  Class 100-10,000
  CMOS integrated circuits
  Microsystems processes
  Nanolithography and nanofabrication
  Back-end CR
  40 m2
  Class 1000-10,000
  Chip packaging
  Hybrid circuit assembly
Integrated Micro and Nano Fabrication Clean Room
Centro Nacional de Microelectrónica

## Slide 7
General Considerations
TCAD Software for (Power) semiconductors
  Silvaco
  Sentaurus
  SRIM (TRIM Monte Carlo simulation)
Previous knowledge:
  Power semiconductor devices: Design, optimisation and fabrication
  Silvaco tools for process technology simulation and Clean Room control
  Sentaurus tools for structure optimisation (selection of optimum geometrical and technological parameters)
  Advanced simulation of device degradation (hot carriers, hot spots, etc.)
  Performance degradation after irradiation of commercial power lateral MOSFETs
  Design and application of Silicon tracking detectors (ATLAS)

## Slide 8
General Considerations
What do we need to simulate / emulate ?
  Radiation hardness of (power) semiconductor devices
    Post-irradiation damage
    Technological modifications to enhance robustness
  Single Event Effects (logic circuits and memories)
    Generated charge profiles
    Transient simulations of complex 3D structures
  Charge generation and evolution in Silicon detectors
    Transient or quasi-static simulation?
    Strategies
  Gain simulation in Silicon detectors

## Slide 9
General Considerations
The interaction between radiation and materials (of a semiconductor device) is based on the moment and energy transfer
  Ionisation damage
  Displacement damage

## Slide 10
General Considerations
Relation between absorbed dose and energy transfer
  Flux (Φ): Number of incident particles (cm-2·s-1)
  Integrated Flux or Fluence (Φ): Total number of incident particles (cm-2)
  Dose (D): Absorbed energy per unit mass (Gray: 1 Gy = 100 J·Kg-1)
  (rad; 1 rad = 100 erg·s-1)
  Stopping Power (S): Energy transfer, normalised to the material density (MeV·cm2·Kg-1)
Ionising Energy Loss (IEL)
Linear Energy Transfer (LET)
Non-Ionising Energy Loss (NIEL)
Total Ionising Dose (TID)
Displacement Damage Dose (DDD)

## Slide 11
Ionisation Damage Simulation

## Slide 12
Ionisation Damage Simulation
The incident particle transfer its energy to a cortical electron, creating an electron-hole pair
The minimum energy to create an electron-hole pair (Shockley theory) is:
The generation rate accounts for the electron-hole pairs created by a TID0 = 1 Rad in 1 cm3
EG (gap), ER (Raman), Ef(Fonons)

## Slide 13
Ionisation Damage Simulation
The damage introduced by the generation of a great amount of electron-hole pairs depends on the transient evolution of the charge and also on the bias and ambient conditions
  Semiconductors:
    If no bias is applied, charge disappears due to recombination. The process is ruled by the carrier lifetimes and does not degrade the material. No simulation interest
    If bias is applied, mobile charge is accelerated by the electric field in the depletion region and a transient current is observed. Single Event Effects
    Transient simulation.
  Dielectrics:
    The number of generated electron-hole pairs is much lower than in semiconductors
    The charge mobility is also much lower than in semiconductors
    As a consequence, carrier are trapped and a certain density of fixed charge is created. Critical in active devices
    Quasi stationary simulation

## Slide 14
Ionisation Damage in Semiconductors

## Slide 15
Ionisation Damage Simulation in Semiconductors
The simulation of ionising particles is only relevant when the density of generated electron-hole pairs is really high (electron-hole plasma)
  Heavy ions typically create an electron-hole plasma
  Transport equation in a non-linear regime have to be solved
  Strong injection conditions are easily reached
  The Sentaurus Heavy Ion model works properly to emulate the transient evolution of the generated charge (Single Event Effects)
    Simulation of particles with Minimum Ionizing Energy is of great interest since the number of generated electron-hole pairs is perfectly known.
    Transient simulations are time costly if accuracy is expected.
    The distribution of the generated electron-hole pairs in the semiconductor has to be previously determined by using a SRIM/TRIM simulator (Stopping and Range of Ions in Matter)

## Slide 16
Single Event Effects: Experimental Study and Simulation
Single Event Effects (SEE):
  Produced by high energy particle hits on sensitive circuit regions
  Main topic in reliability and device performance in space applications
Study and prediction of SEE require test in particle accelerator facilities
  Heavy Ion accelerator provide high energy capabilities
  High cost and limited availability impose alternative methodologies
Numerical simulation techniques are able to predict device and circuit behaviour after an ion hit

## Slide 17
Single Event Effects: Experimental Study and Simulation
Physics of the incident particle and its interaction with matter (SRIM-Stopping and Rang of Ions in Matter):
  Calculations on the energy deposition of ions passing through matter
  Linear Energy Transfer (LET) profile along the particle track can be obtained
Electric performance of the circuit after the perturbation (CADENCE-SPECTRE):
  Perturbation is replaced by a pulsed current in the affected node
  Single Event evolution can be followed
Semiconductor solid state physics (Synopsys Sentaurus TCAD):
  Exact reproduction of the charge collection phenomenology
  Accurate consequences over the electrical characteristics can be evaluated
Simulation Techniques: Different Approaches.

## Slide 18
Ionisation Damage in Oxides
Case Study: Power LDMOS Transistor

## Slide 19
Ionisation Damage Simulation in Oxides
Two approaches can be contemplated:
  Simulation of the defect evolution
    Transport, anneal and recombination models
    Transient simulation (time costly)
    Continuity equations are not solved in oxides
      “Oxide as semiconductor” option has to be selected and a correct set of parameters have to be introduced (good knowledge of the dielectric)
  Simulation of the permanent damage using Sentaurus Fixed Charge and Traps models
    Quasi-static simulation
    Average final values necessary
  A relation between defects and Dose (TID) is needed
    Generation of fixed charge (Not) and interface traps (Nit)
    Energy distribution of traps (Dit)
    Strong electric field dependence (irradiation bias conditions to be emulated)

## Slide 20
Ionisation Damage Simulation in Oxides
Calculation of the recombination efficiency (fy)
  Efficiency of the recombination process (fy) is the ratio between surviving holes and total generated holes
  Recombination strongly depends on the ionising particle
                X or γ rays (60Co) generate charges in almost all the dielectric volume (Slow recombination)
                α particles generate charges in the neighbourhood of their trajectory (Fast recombination)
  The efficiency of the recombination also depends on the electric field
    For 60Co: m=0.7 and E1=0.55 MV/cm

## Slide 21
Ionisation Damage Simulation in Oxides
Charge generation and evolution in a MOS structure
  Electron-hole pairs suffer an initial recombination (low electric field)
  Under high electric field electrons are immediately removed through the gate electrode
  Holes are also drift by the high electric field, but their mobility is low and take time to reach the Si/SiO2 interface (hopping transport)
  Some holes are trapped in the deep levels at the region close to the Si/SiO2 interface creating fixed charges and interface traps

## Slide 22
Ionisation Damage Simulation in Oxides
Calculation of the trapping efficiency (fot) and fixed charges (Not)
  Survivor holes (to the eventual initial recombination) travel through the oxide
  Holes can be trapped in their way to the oxide interface
  The efficiency of the trapping process (fot) is the ratio between trapped holes and surviving holes
    The trapping efficiency depends on the electric field and on the oxide quality
    If the oxide thickness is lower than 15 nm, holes are completely removed by tunneling effect (fot=0)
  Finally:
    The fixed charges are described by
Initially generated

## Slide 23
Calculation of the Interface traps
  Traps in the Si/SiO2 interface are related with the H+ density in the oxide (depends on the growth process) and are identified as Pb
    Incident particles release H+ which are drift to the Si/SiO2 interface where they create dangling bonds (traps)
  Finally:
    The interface traps (Nit) are described by
    (where ait is the kinetic constant and p is the H+ concentration)
    Nit can also be expressed as a function of the ionising dose (TID) as
    (where bit depends on the process technology and is determined by
    performing tests on capacitors. Typically bit~1)
  Only two energy levels are considered: EV+0.3 eV (acceptor) and Ev+0.8 eV (donor)
Ionisation Damage Simulation in Oxides

## Slide 24
Ionisation Damage Simulation Procedure in Oxides
Fixed charge (Not) is introduced in Sentaurus by setting the charge parameter
Traps in the Si/SiO2 interface are set by:
  The two energy levels (EV+0.3 eV and Ev+0.8 eV)
  The superficial trap concentration (Nit)
  Capture cross-section of electrons and holes

## Slide 25
Ionisation Damage in LDMOS Transistors
LDMOS transistors will be used in DC-DC converters for the HL-LHC upgrade
  Transistors from IHP Microelectronics (DE) (0.25 µm SGB25V GOD SiGe BiCMOS)
  Submitted to neutron irradiation (0.5, 5 and 10 Mrad)
First step: Technological and electrical simulation of basic cell and fitting with experimental data
Second step: Electric field distribution (oxides and semiconductors)
VBD = 22 V, fT = 20 GHz
VBD = -16 V, fT = 10 GHz

## Slide 26
Ionisation Damage in LDMOS Transistors
Third step: Definition of oxide blocks for fixed charge and interface traps
Fourth step: Calculation of recombination efficiency fy(Eox) and fixed charges Not (fot has to be tuned with available irradiation data)
  Not values are introduced in Sentaurus as fixed charges in each oxide block
Fifth step: Calculation of interface traps Nit according to:
(ait has to be tuned with available irradiation data)
fot and ait values according to available irradiation data

## Slide 27
Ionisation Damage in LDMOS Transistors
Not effect
Nit effect

## Slide 28
Ionisation Damage in LDMOS Transistors
Accurate fitting between simulated and measured IDS versus VDS curves

## Slide 29
Displacement Damage

## Slide 30
Displacement Damage Simulation
Displacement damage in oxides is not relevant (only optical effects)
Displacement damage in semiconductors creates energy levels in the gap
  Minority carrier lifetime reduction
  Reduction of carriers (n or p)
  Mobility degradation
Edispl = Minimum energy for atomic dislocation
Edispl-th = Minimum energy for relevant displacement damage

## Slide 31
Displacement Damage Simulation Procedure
Sentaurus includes a model for Semiconductor Traps
Typical traps in Float Zone substrates for Silicon detectors are perfectly determined
  The total trap concentration (Nt) is the added contribution of filled (nt) and empty (pt)
  (where η is the introduction rate, determined by DLTS measures)
  The effective doping concentration in the P-type substrate is finally given by:
University of Peruggia model, including Pennicard corrections

## Slide 32
Displacement Damage in MOS Capacitors
Simulation of displacement damage in MOS capacitors under 24 GeV proton irradiation conditions
  The introduction rate (η) is calculated for the equivalent 1 MeV neutrons. Hence, the fluence has to be corrected according to the 24 GeV protons
Boron concentration = 8e14 cm-3
Oxide thickness = 10 nm

## Slide 33
Case Study: Design of
Low Gain Avalanche Photodetectors

## Slide 34
PiN Diodes
  Proportional response
  Good efficiency
  Good spectral range
  Segmentation is technologically available (strip and pixel detectors).
  After Irradiation
  Worse signal to noise ratio (lower quality signal + noise increment)
  Increment of the power consumption (leakage current increase)
  Ionisation damage (relevant on n-on-p structures)
Low Gain Avalanche Detectors (LGAD)
  Proportional response (linear mode operation)
  Good efficiency
  Good spectral range
  Better sensibility (Gain)
  Thin detector integration with the same signal and higher collection efficiency
  Better signal/noise ratio
  After Irradiation
  Similar pre & post irradiation signal (higher quality signal + lower noise increase)
  Power consumption slightly increased
  Ionisation damage in oxides (relevant on n-on-p structures)
Silicon Detectors with Internal Gain and Proportional Response
Tracking Detectors
  Internal Gain
Notes: The aim of this work is to improve the performance and stability against radiation of PiN diode detectors for tracking applications.
In this sense, the controlled use of avalanche phenomenon, characteristic of a PN junction polarized in reverse mode, allow us to improve some characteristics of the PiN diodes used in such applications.
Thus, we will be able to get more stable detectors, reducing degradation due to radiation, and achieving a higher signal to noise ratio. This will allow more accurate detection of the particles and the fabrication of thinner detectors with the same signal and greater collection efficiency.

## Slide 35: Linear Mode Operation. Gain Definition
Diodes with multiplication can operate in Linear or Geiger mode
  Linear mode: Moderate gain: Proportional response to the deposited energy
  Geiger mode: Very high gain: Digital response (detection or not detection)
[1] A.G. Stewart et al. in Proc. of SPIE, Vol. 6119, 2006
No Gain
Moderate Gain
&
Proportional response
Gain > 104
Digital response
Linear mode
Notes: Since we are interested in a detector with a moderate gain and a proportional response, we fix its operating point in the linear region with a voltage below its breakdown voltage.
In this situation, we consider the Gain as the ratio between the signal at this point and the constant signal at low voltage, taking into account the procedure fixed by Tapan in 1997.

## Slide 36: PiN Diode (No Gain)
P-type (π)substrate
N+ cathode
P+ anode
Abrupt N+P junction with trapezoidal electric field profile (linearly decreasing in the P substrate)
  Electrons are accelerated towards the N+ region until they reach the saturation velocity
  Since the electric field is much lower than Ecrit, electrons can not generate new carriers
  (no impact ionisation and no gain)
Notes: The structure on which we have worked is based on a PiN-PAD diode with an area of 25 square millimeters.

## Slide 37: Pad Diode with internal Gain
P-type (π)substrate
P-type multiplication layer
N+ cathode
P+ anode
Gaussian N+P junction where the P-multiplication layer becomes completely depleted at a very low reverse voltage
  Electrons are accelerated towards the N+ region until they reach the saturation velocity
  The electric field in the P layer is close to the Ecrit, value (impact ionisation and gain)
Notes: On a highly resistive P-type substrate, prior to N-plus well to form the diffusion cathode, we have defined a P well to be the multiplication layer. The objective of this layer is to enhance the value of the electric field in that region, and its impurity profile will be the main technological parameter to define in order to adjust the gain value.

## Slide 38: Conditions for Gain
Impact ionisation requires a minimum electric field of 1e5 V/cm in the P layer
  Full depletion of the P-type substrate is needed to avoid recombination
  The Ecrit value (~3e5 V/cm) can not be reached in the N+P junction (reverse breakdown)
Impact ionisation region
Electrons traveling at their saturation velocity (good for signal uniformity)

## Slide 39: Gain Definition and Usage
The Gain can be defined in two equivalent ways and is identical whatever the incident particle is
  A known radiation source has to be used to calibrate the gain
    Collected charge is determined by integrating the current waveform
    The total number of generated electron-hole pairs in Silicon is determined by the type of radiation source
If no impact ionisation is contemplated (Equivalent PiN diode.)
Once the Gain is calibrated, the detector can be used to identify the incident radiation by simply measuring the collected charge

## Slide 40: Gain Simulation
Gain simulation considering generated and collected charge
  An initial charge distribution has to be introduced in the Sentaurus Heavy Ion model
  The evolution of the generated charge is calculated by transient simulations
  We have not been able to observe any transient current increase
    Impact ionisation is an statistic concept while transient simulation considers the evolution of each single electron…
Gain simulation considering multiplied and non-multiplied current (alternative method)
  Ionisation coefficients are modified in a very small volume of the P-type substrate (3 orders of magnitude greater) to create a know number of electron-hole pairs (3000)
  Quasi static simulations are performed with and without the generated charge
    The PiN diode is simulated to determine current increase due to the generated charge (no impact ionisation is present)
    Then, the LGAD counterpart is simulated with and without charge (impact ionisation is present)
    Finally, the simulated Gain corresponds to the ratio between PiN and LGAD currents when charge is generated

## Slide 41: Gain Simulation

## Slide 42: Gain Simulation
  Local charge generation equivalent to the absorption of a 30 KeV X-ray
  The doping of the sample B P-multiplication layer is higher than the A sample (high Gain)

## Slide 43: Design of the P-Multiplication Region
If implant dose increases:
  Gain increases
  VBD decreases
Small modifications in the Boron implant dose (~ 2 × 1012 cm-2) induce great changes in Gain and VBD
1D Simulation @ Pad Centre
Gain/VBD trade-off
Doping profile of the P-multiplication layer is critical
Notes: The simulations show that the adjustment of the impurity profile in this region is critical, due to its effect on the gain and on the voltage capability for the analyzed detector. The P well dose must be enough to obtain a determined gain without a high reduction on its breakdown voltage.
Thus, small modifications in the Boron implant dose, in the order of ten to twelve atoms per square centimeter, can induce great changes on the gain and breakdown voltage values.
Therefore, the accurate control of the doping profile in the multiplication area, is the most important technological condition for its fabrication.

## Slide 44: Design of the Edge Termination
P-Multiplication layer
P-Substrate
The optimisation of the edge termination is ruled by the electric field at the multiplication layer (not by the maximum voltage capability, as in the case of power devices)
Correlated values

## Slide 45: Edge Termination: Why is needed?
The N+ shallow contact and the P-multiplication layers have to be locally created with a lithography mask
  The electric field at the curvature of the N+/P junction is much higher than that of the plane junction (where Gain is needed)
  Avalanche at the N+/P curvature at a very low reverse voltage (premature breakdown)
Shallow N+ and P-multiplication layers self aligned
High electric field peak at the curvature

## Slide 46: Compatible Edge Termination Techniques
Maximum efficiency of 90%
Maximum efficiency of 80%
Maximum efficiency of 60%

## Slide 47: Edge Termination with Guard Ring
The N+ shallow diffusion is used to implement a floating guard ring
  The lateral electric field distribution is smoothed leading to two peaks (main junction and floating guard ring)
  The electric field peak and the risk of avalanche breakdown at the curvature of the main junction is reduced. Optimisation of the guard ring location is needed

## Slide 48: Edge Termination with N+ Extension
The N+ shallow diffusion is used to extend the N+ beyond the edge of the multiplication layer
  Phosphorous diffuses more in the very low doped substrate (higher curvature radius and voltage capability)
  The electric field rapidly increases at the plain junction (multiplication)
  At high reverse voltage the electric peak at the extended N+ diffusion leads to avalanche breakdown
Multiplication
Avalanche

## Slide 49: Edge Termination with Junction Termination Extension
P-type substrate
N+ cathode
P+ anode
JTE diffusion
P-type multiplication layer
Junction Termination Extension (JTE) with an additional deep N diffusion
  Additional photolithographic step with high energy Phosphorous implantation
  A field plate can also be implemented for additional electric field smoothing
Field Plate
Notes: To achieve this condition, we define a low doping N-well in the periphery of the cathode diffusion, deeper than this, and with the aim to increase the voltage cability of the peripheral zone. This low doping N-well is known as Junction Termination Extension (JTE).

## Slide 50: Edge Termination with Junction Termination Extension
  Deep N diffusion with high curvature radius (long anneal process)
  Reduced electric field peak at the JTE diffusion
  Highest electric field at the plane junction (gain control) VBD plane < VBD JTE (Gain control)
Multiplication and avalanche control

## Slide 51: Edge Termination with Junction Termination Extension
N+
P
N
π
Electric Field @ 400 V
Planar and uniform electric field distribution, high enough to activate charge multiplication
Notes: The reduction in the peripheral electric field, allows that the maximum Electric Field is reached in the multiplication area. We can also see how, if we add a field plate on the end of the JTE, we can increase the reduction of the electric field, increasing the breakdown voltage in that area.

## Slide 52: Design of the Device Periphery
  Full depletion below 100 V reverse bias
  Fast lateral depletion of the low doped substrate (A deep P+ diffusion –P stop- is needed in the die periphery to avoid the depletion region reaching the unprotected edge

## Slide 53: What about the Inherent Positive Oxide Charges?
  Field oxides grown in wet conditions (H2+O2) typically have a positive charge density in the range of 5e10 cm-2
  Surface inversion and modification of the depletion region, reaching the deep P-Stop peripheral diffusion
Surface inversion + fast depletion + electric field peak at deep P-stop+ SURFACE LEAKAGE CURRENTS

## Slide 54: How to Protect the Surface, Limiting the Current Leakage?
Oxide positive charges create a surface inversion layer (electron path towards the cathode electrode, masking the charge collection when used as a detector)
  A shallow P-type diffusion (P-Spray) can be used to compensate the surface inversion
  A deep P+ diffusion can be placed close to the JTE to eliminate the electron surface current
Blanket Boron implantation
Same Boron implantation

## Slide 55: How to Protect the Surface, Limiting the Current Leakage?
An additional N-type ring is implemented by using the deep JTE diffusion
  The N ring has to be placed close to the JTE to avoid a premature breakdown at the JTE
  The P-spray diffusion has to be efficient (to avoid short circuit through the inversion layer)
  The voltage capability is not degraded since the junction to be protected is now the right edge of the added ring (identical than the JTE)
N
N+
P+
P
N
N+
Multiplier Junction
Overlap
Collector Ring
P-

## Slide 56: Simulation of the Irradiated Devices
High Electric Field peak at the junction
No Irradiated
Irradiated. Φeq = 1 x 1015
PiN: electric field strength at the junction increases after irradiation
LGAD: electric field strength at the junction is almost equal after irradiation
Irradiation Trap Model (Perugia Model)
Acceptor; E= Ec + 0.46 eV; η=0.9 σe = 5 x 10-15 σh = 5 x 10-14
Acceptor; E= Ec + 0.42 eV; η=1.613 σe = 2 x 10-15 σh = 2 x 10-14
Acceptor; E= Ec + 0.10 eV; η=100 σe = 2 x 10-15 σh = 2.5 x 10-15
Donor; E= Ev - 0.36 eV; η=0.9 σe = 2.5 x 10-14 σh = 2.5 x 10-15
Curves @ 600 V
Impact Ionization Model (Univ. of Bolonia)
Notes: Taking into account that the value of the electric field in the junction, causes the appearance of the charge multiplication, using numerical simulations we can compare the electric field profile of an irradiated detector with an un-irradiated one.
Thus, simulations show that the electric field at the junction of a PiN diode increases by the action of radiation, while maintaining substantially equal in the low gain avalanche diode (LGAD).

## Slide 57: Experimental Results
Wafer 5 (1.4 × 1013 cm-2)
W5_F11
Current level
(~ few hundreds of nA)
Junction breakdown above 1100 V
Static Performance
  Current levels below 1 µA thorough the whole voltage range
  Junction breakdown above 1100 V
Notes: In all cases identified as "good devices", the reverse leakage current is less than one micro ampere for voltages lower than the breakdown voltage. This voltage reaches a value of eleven hundred volts for all wafers (1100 V), except the eighth wafer that reaches eight hundred volts, as planned.

## Slide 58: Experimental Results
Multiplication factor has been tested with tri-alpha (239Pu/241Am/244Cm) source.
  Irradiation through the anode (back side, 1 µm Aluminum):
Back Side Irradiation
Notes: The Detectors characterization using a tri-alpha source, shows how the gain increases with voltage, which is in the range of 10.
Irradiation measures through the back of the detector, provide better results than the measurements performed irradiating through the cathode.

## Slide 59
Notes: That's all. Thank you very much for your attention.